ME-MS81h

High grade Rare Earth elements by fusion/ICPMS

Sample Decomposition:

Lithium Metaborate Fusion (FUS-LI01h)

Analytical Method:

Inductively Coupled Plasma - Mass Spectroscopy (ICP - MS)

A prepared sample (0.100 g) is added to lithium metaborate flux (0.90 g), mixed well and fused in a furnace at 1000°C. The resulting melt is then cooled and dissolved in 250 mL of 4% nitric acid. This solution is then analyzed by inductively coupled plasma - mass spectrometry.

| Element | Symbol | Units | Lower Limit | Upper Limit |
| --- | --- | --- | --- | --- |
| Cerium | Ce | ppm | 3 | 50000 |
| Dysprosium | Dy | ppm | 0.3 | 5000 |
| Erbium | Er | ppm | 0.2 | 5000 |
| Europium | Eu | ppm | 0.2 | 5000 |
| Gadolinium | Gd | ppm | 0.3 | 5000 |
| Hafnium | Hf | ppm | 1 | 50000 |
| Holmium | Ho | ppm | 0.05 | 5000 |
| Lanthanum | La | ppm | 3 | 50000 |
| Lutetium | Lu | ppm | 0.05 | 5000 |
| Niobium | Nb | ppm | 1 | 5000 |
| Neodymium | Nd | ppm | 0.5 | 50000 |
| Praseodymium | Pr | ppm | 0.2 | 5000 |
| Rubidium | Rb | ppm | 1 | 50000 |
| Samarium | Sm | ppm | 0.2 | 5000 |
| Tin | Sn | ppm | 5 | 50000 |
| Tantalum | Ta | ppm | 0.5 | 5000 |
| Terbium | Tb | ppm | 0.05 | 5000 |
| Thorium | Th | ppm | 0.3 | 5000 |
| Thulium | Tm | ppm | 0.05 | 5000 |
| Uranium | U | ppm | 0.3 | 5000 |
| Tungsten | W | ppm | 5 | 50000 |
| Yttrium | Y | ppm | 3 | 50000 |
| Ytterbium | Yb | ppm | 0.2 | 5000 |
| Zirconium | Zr | ppm | 10 | 50000 |

Elements listed below are available upon request

| Element | Symbol | Units | Lower Limit | Upper Limit |
| --- | --- | --- | --- | --- |
| Indium | In | ppm | 0.3 | 5000 |