Sample Preparation – Pulverizing Procedures PUL-3kg

Pulverize up to 3 kg of raw sample

Analytical Method:	‘Flying Disk’ or ‘Ring and Puck’ style grinding Mill

A sample up to 3 kg is ground in a ring mill pulverizer using a standard low chrome steel ring set. If the sample is > 3 kg, it is split prior to pulverizing and the remainder may be retained or discarded. Samples too coarse to be put directly into a pulverizing mill, or where the particle size needs to be reduced before a representative split can be taken will be crushed and split prior to pulverizing. The remainder may be saved or dumped at the client’s request.

| Method Code | Mass | Specifications | Description |
| --- | --- | --- | --- |
| PUL-23 | ≤ 3 kg | 85 % < 75 m | Pulverize up to 3 kg of raw sample. Samples > 3 kg are split prior to pulverizing and the remainder retained. |
| PUL-24 | ≤ 3 kg | 85 % < 75 m | Pulverize up to 3 kg of raw sample. Samples > 3 kg are split prior to pulverizing and the remainder discarded. |
| PUL-25 | ≤ 3 kg | 85 % < 75 m | Pulverize up to 3kg of raw sample. Samples > 3 kg are crushed and split prior to pulverizing and the remainder retained. |
| PUL-26 | ≤ 3 kg | 85 % < 75 m | Pulverize up to 3 kg of raw sample. Samples > 3kg are crushed and split prior to pulverizing and the remainder dumped. |
| PUL-QC | 25 g | See method specifications | Testing procedure for ring pulverized material. |

Note: All grinding surfaces impart some degree of metal content to samples during preparation. Please review our technical note “Contamination Introduced by Sample Preparation Equipment” for further information.