Crushing Procedures

The entire sample is passed through a primary crusher to yield a crushed product which passes the screen specifications of the designated crushing procedure.  A split, (split size is determined by the final preparation method and analysis requested), is then taken.

| Method Code | Specifications | Description |
| --- | --- | --- |
| CRU-21 | 70 % < 6 mm | Coarse crushing of rock chip and drill samples to better than 70 % of the sample passing 6 mm. |
| CRU-31 | 70 % < 2 mm | Fine crushing of rock chip and drill samples to better than 70 % of the sample passing 2 mm. Standard preparation for samples where a representative split will be pulverized. |
| CRU-32 | 90 % < 2 mm | Fine crushing of rock chip and drill samples to better than 90 % of the sample passing 2 mm. Applicable to samples that exhibit coarse gold effects. |
| CRU-33 | 95 % < 2 mm | Fine crushing of rock chip and drill samples to better than 95 % of the sample passing 2 mm. |