ME-ICP61

Trace Level Methods Using Conventional ICP-AES Analysis

Sample Decomposition:

HNO3-HClO4-HF-HCl digestion, HCl Leach (GEO-4ACID)

Analytical Method:

Inductively Coupled Plasma - Atomic Emission Spectroscopy (ICP - AES)

A prepared sample (0.25 g) is digested with perchloric, nitric, hydrofluoric and hydrochloric acids. The residue is topped up with dilute hydrochloric acid and the resulting solution is analyzed by inductively coupled plasma-atomic emission spectrometry. Results are corrected for spectral interelement interferences.

NOTE: Four acid digestions are able to dissolve most minerals; however, although the term “near-total” is used, depending on the sample matrix, not all elements are quantitatively extracted.

| Element | Symbol | Units | Lower Limit | Upper Limit | Default Overlimit Method |
| --- | --- | --- | --- | --- | --- |
| Silver | Ag | ppm | 0.5 | 100 | Ag-OG62 |
| Aluminum | Al | % | 0.01 | 50 |  |
| Arsenic | As | ppm | 5 | 10000 |  |
| Barium | Ba | ppm | 10 | 10000 |  |
| Beryllium | Be | ppm | 0.5 | 1000 |  |
| Bismuth | Bi | ppm | 2 | 10000 |  |
| Calcium | Ca | % | 0.01 | 50 |  |
| Cadmium | Cd | ppm | 0.5 | 500 |  |
| Cobalt | Co | ppm | 1 | 10000 | Co-OG62 |
| Chromium | Cr | ppm | 1 | 10000 |  |
| Copper | Cu | ppm | 1 | 10000 | Cu-OG62 |
| Iron | Fe | % | 0.01 | 50 |  |
| Gallium | Ga | ppm | 10 | 10000 |  |
| Potassium | K | % | 0.01 | 10 |  |
| Lanthanum | La | ppm | 10 | 10000 |  |
| Magnesium | Mg | % | 0.01 | 50 |  |
| Manganese | Mn | ppm | 5 | 100000 |  |
| Molybdenum | Mo | ppm | 1 | 10000 | Mo-OG62 |
| Sodium | Na | % | 0.01 | 10 |  |
| Nickel | Ni | ppm | 1 | 10000 | Ni-OG62 |
| Phosphorus | P | ppm | 10 | 10000 |  |
| Lead | Pb | ppm | 2 | 10000 | Pb-OG62 |
| Sulphur | S | % | 0.01 | 10 |  |
| Antimony | Sb | ppm | 5 | 10000 |  |
| Scandium | Sc | ppm | 1 | 10000 |  |
| Strontium | Sr | ppm | 1 | 10000 |  |
| Thorium | Th | ppm | 20 | 10000 |  |
| Titanium | Ti | % | 0.01 | 10 |  |
| Thallium | Tl | ppm | 10 | 10000 |  |
| Uranium | U | ppm | 10 | 10000 |  |
| Vanadium | V | ppm | 1 | 10000 |  |
| Tungsten | W | ppm | 10 | 10000 |  |
| Zinc | Zn | ppm | 2 | 10000 | Zn-OG62 |

Elements listed below are available upon request

| Element | Symbol | Units | Lower Limit | Upper Limit | Default Overlimit Method |
| --- | --- | --- | --- | --- | --- |
| Lithium | Li | ppm | 10 | 10000 |  |
| Niobium | Nb | ppm | 5 | 2000 |  |
| Rubidium | Rb | ppm | 10 | 10000 |  |
| Selenium | Se | ppm | 10 | 1000 |  |
| Tin | Sn | ppm | 10 | 10000 |  |
| Tantalum | Ta | ppm | 10 | 10000 |  |
| Tellurium | Te | ppm | 10 | 10000 |  |
| Yttrium | Y | ppm | 10 | 10000 |  |
| Zirconium | Zr | ppm | 5 | 500 |  |