Suite 6

642 Albany Hwy

Victoria Park

WA 6100

Client:	Reward Minerals Ltd

Job number: 	11_062

Sample:	11_062_03

Client ID:	T600 RJ PH3 XTAL 220111

Date:	17/2/11

Analysis:	Qualitative mineralogical analysis by x-ray diffraction (XRD)

Sample Preparation

The sample was supplied to Microanalysis Australia as fine grained, white crystalline powder. A representative sub –sample was removed and lightly ground such that 90% was passing 20 µm. Grinding to this size helps eliminate preferred orientation.

Analysis

Only crystalline material present in the sample will give peaks in the XRD scan. Amorphous (non crystalline) material will add to the background. The search match software used was Xplot. An up to date ICDD card set was used. The x-ray source was cobalt radiation.

No standards were used in the semi-quantitative interpretation. The peak area integration method was used whereby the 100% peak areas for each phase are summed and the relative contribution of each mineral phase calculated as it’s percentage of the sum.

Summary

The phases are listed in order of interpreted concentration:

| Mineral phase | Concentration (%) | ICDD match probability |
| --- | --- | --- |
| Halite (NaCl) | 89.0 | Good |
| Thenardite (Na2SO4) | 9.0 | Good |
| Blodite (Na2Mg(SO4)2•4H2O) | 2.0 | Good |

The ICDD match probability is reported as an indication as to how well the peak positions and relative intensities for the sample matched those in the published literature (www.icdd.org) for that particular compound.